IONIC FILM MANUFACTURING PROCESS FLOWCHART

Salt Electro Mining Technology (SEM TECH)

Rowow LLC - 2026

NOTE: Plain-text companion to Ionic-Film-Manufacturing-Process-Flowchart.docx

For the full formatted flowchart with diagrams, open the .docx file.

================================================================================

OVERVIEW

================================================================================

This document outlines the step-by-step manufacturing process for fabricating a

low-cost, homogeneous ion exchange membrane (ionic film) from off-the-shelf

precursor materials. No specialized industrial equipment required.

The ionic film serves as the selective ion transport layer in Rowow LLC's

closed-loop electrochemical precious metal recovery system (SEM TECH).

================================================================================

MATERIALS REQUIRED

================================================================================

Primary Materials:

- Ion exchange water softener resin (sulfonated polystyrene beads)

- PVC cement (contains THF + PVC polymer in solvent)

- Methylene blue dye (optional - for cation selectivity testing)

Equipment:

- Mortar and pestle (or blender/grinder)

- Flat glass surface or silicone mat

- Spatula or palette knife

- Safety: nitrile gloves, eye protection, ventilation

================================================================================

MANUFACTURING STEPS

================================================================================

PHASE 1 - RESIN PREPARATION

Step 1: Obtain granular cation exchange resin (water softener type)

Step 2: Dry resin - air-dry 24-48h or oven at 60C for 2-4h

Step 3: Pulverize to fine powder (target < 200 micron particle size)

PHASE 2 - BINDER MIXING

Step 4: Use PVC cement as-is (work in ventilated area - THF fumes)

Step 5: Mix resin powder + PVC cement at ~70% resin : 30% cement (by volume)

until a thick, homogeneous paste forms

Step 6: Adjust consistency - too thick: add cement; too thin: add resin

PHASE 3 - FILM CASTING

Step 7: Place silicone mat or glass on level surface

Step 8: Spread paste to uniform 0.5-2mm thickness

Step 9: Allow THF solvent to evaporate - do not disturb for 30-60 min

PHASE 4 - CURING

Step 10: Cure 24h at room temperature (or 4-6h at 40-50C)

Step 11: Peel film, inspect for cracks/bubbles, trim edges

Step 12: Soak in DI water or 0.1M NaCl for 1-4h to hydrate ion groups

PHASE 5 - QUALITY TESTING

Step 13: Visual inspection - uniform, flexible, no large defects

Step 14: Conductivity test - measure ionic conductivity vs. control

Step 15: Selectivity test - methylene blue dye test (cation membrane blocks dye)

================================================================================

ANION EXCHANGE MEMBRANE VARIANT

================================================================================

Substitute anion exchange resin (quaternary ammonium type) for cation resin.

Same PVC cement binder and casting process applies.

================================================================================

TROUBLESHOOTING

================================================================================

Cracks during drying   -> Increase PVC cement ratio; dry more slowly

Brittle film           -> Add more PVC cement; ensure full hydration

Poor conductivity      -> Increase resin content; reduce thickness; check hydration

Film sticks to surface -> Use release agent; allow full cure before peeling

================================================================================

SAFETY NOTES

================================================================================

- THF (in PVC cement) is highly flammable. Keep away from flames.

- Work in well-ventilated area or use respiratory protection.

- Wear nitrile gloves (THF penetrates latex).

- Dispose of THF waste per local regulations.

- Resin dust: avoid inhalation.

================================================================================

RESOURCES

================================================================================

Full technical docs:  Rowow-LLC-Technical-Volume.pdf

Membrane diagrams:    Ionic-Film-Manufacturing-Process-Flowchart.docx

Patent filing:        Patent.pdf

YouTube @Rowow:

CATION membrane build: https://www.youtube.com/watch?v=40wbNGVR3Xw

Electrolysis cells:     https://www.youtube.com/watch?v=vx_uQVsYAuo

Website:   https://rowow.net

Discord:   https://discord.gg/e7CmU2ekky

GitHub:    https://github.com/Rowow-LLC

================================================================================

LICENSE

================================================================================

CERN-OHL-S v2 - CERN Open Hardware Licence Version 2 - Strongly Reciprocal

Free to use, copy, modify, make, and sell, on the condition that you

release your version's full design source under the same license.

See LICENSE file for full terms.

Rowow LLC - Florida, USA - https://rowow.net